## Slide 1
PHY 752 Solid State Physics
11-11:50 AM MWF Olin 103
Plan for Lecture 8:
    Reading: Chap. 2 in GGGPP;
    Conclude brief introduction to group theory
      Compatibility relations for representations
      Crystal field splitting
      International Tables for Crystallography

## Slide 3
The great orthogonality theorem
Results from last time --

## Slide 4
Results from last time -- continued
Character orthogonality theorem:
Number of elements in class C

## Slide 5
Summary of relationships between the characters and classes of a group which follow from the great orthogonality theorem
These results also imply that the number of classes is the same as the number of characters in a group.

## Slide 6
Example character table for cubic group corresponding to point symmetry of Brillouin zone at k=0

## Slide 7
purely periodic

## Slide 8
How do states at k=0 “connect” with states with

## Slide 9
Band structure diagram for fcc Cu (Burdick, PR 129 138-159 (1963))

## Slide 11
Example
D | E | C42 | 2C4 | 2JC42 | 2JC2
G25’ | 3 | -1 | -1 | -1 | 1
D2’ | 1 | 1 | -1 | -1 | 1
D5 | 2 | -2 | 0 | 0 | 0

## Slide 12
Use of character table analysis in crystal field splitting
  Question: What happens to a spherical atom when placed in a crystal?
The group which describes the general rotations in 3-dimensions has an infinite number of members, but an important representation of this group is the matrix which rotates to coordinate system about the origin R, transforming

## Slide 13
Analysis of the 3-dimensional rotation group -- continued

## Slide 14
Compatibility of continuous rotation group with the cubic group:
l=0 1 1 1 1 1 1 1 1 1 1
l=1 3 -1 1 -1 0 -3 1 -1 1 0
l=2 5 1 -1 1 -1 5 1 -1 1 -1

## Slide 15
l=0 1 1 1 1 1 1 1 1 1 1
l=1 3 -1 1 -1 0 -3 1 -1 1 0
l=2 5 1 -1 1 -1 5 1 -1 1 -1
G1
G15
G12+G25’

## Slide 16
Visualization of l=2 orbitals from http://chemwiki.ucdavis.edu/Inorganic_Chemistry/Crystal_Field_Theory/Crystal_Field_Theory
G12
G25’
Octahedral symmetry

## Slide 17
Octahedral symmetry effects on d-orbitals
Energy diagram
G12 =eg
G25’=t2g

## Slide 18
Comment on representation notations for cubic group

## Slide 19
Tetrahedral symmetry effects on d-orbitals
G12 =eg
G25’=t2g

## Slide 20
Symmetry information available in the
International Tables for Crystallography
http://it.iucr.org/