## Slide 1
Li3BO3 and Li3BN2: Computational Study of Structural and Electrolyte Properties of Pure and Doped Crystals
Yan Li1, Zachary D. Hood2, Natalie A. W. Holzwarth1
1Department of Physics, Wake Forest University, Winston-Salem, NC 27109, USA
2Applied Materials Division, Argonne National Laboratory, Argonne, IL 60439, USA
APS March Meeting 2021
Session E61: Energy Research -- Energy Storage I

## Slide 2
Outlines
β-Li3BN2
Monoclinic P21/c (#14)2
4 formula units / unit cell
γ-Li3BN2
Tetragonal I41/amd (#141)3
8 formula units / unit cell
1Stewner, Acta Crystallogr. section B. 27, 904 (1971)
2Yamane et al., J. Solid State Chem. 71, 1-11 (1987)
3Pinkerton and Herbst, J. Appl. Phys. 99, 113523 (2016)
Inequiv. Li
B
N
α-Li3BN2
Tetragonal P42/mnm (#136)2
2 formula units / unit cell
Li3BO3
Monoclinic P21/c (#14)1
4 formula units / unit cell
O
Focuses of this presentation:
Structure correction for α-Li3BN2
Electrolyte properties of pure and doped Li3BO3 and β-Li3BN2 crystals
Stability analysis of the ideal interfaces of pure Li3BO3 and β-Li3BN2 with Li metal anode

## Slide 3
Density Functional Theory (DFT) and Density Functional Perturbation Theory (DFPT) with the modified Perdew-Burke-Ernzerhof generalized gradient approximation1 (PBEsol GGA)
The projector augmented wave (PAW) formalism using ABINIT (https://www.abinit.org) & QUANTUM ESPRESSO (http://www.quantum-espresso.org)
Datasets generated by ATOMPAW code available at http://pwpaw.wfu.edu
Visualization software: XCrySDen, VESTA
Space-group analysis: FINDSYM
X-ray diffraction: Mercury
Summary of computational methods
1Perdew et al., Phys. Rev. L. 100, 136406 (2008)

## Slide 4
Corrected α phase of Li3BN2
Li(4d)
Li(2b)
Modes #1&2 at M (0.5, 0.5, 0)
Li(8g)
Li(2a)
Li(2b)
Distort b-type Li ions along c
Orthorhombic Pmmn
Super tetragonal P42/mnm
New α-Li3BN2 in the Pmmn structure
Reported α-Li3BN2 in the P42/mnm structure
Brillouin zone diagrams: Hinuma et al., Comp. Mat. Sci. 128, 140-184 (2017)

## Slide 5
Comparison of simulated and experimental x-ray diffraction (λ = 1.54056 A° ) patterns.
Harmonic vs. Quasi-harmonic
Exp: Yamane et al., J. Solid State Chem. 71, 1-11 (1987)

## Slide 6
Defect models for monoclinic Li3BO3 and β-Li3BN2
Inequiv. host Li
interstitial Li
3x1x1 supercell of Li3BO3 (P21/c)
Models of Li-deficient structures:
Pure crystal with an ideal Li vacancy created by removing a Li ion and compensating with a uniform charge of the opposite sign -- I-vac
F-doped crystal with the stoichiometry of Li3-xBO3-xFx (x = 1/12) -- F-doped
C-doped crystal with the stoichiometry of Li3-xB1-xCxN2 (x = 1/16) -- C-doped
Stability analysis:
Metastable interstitial defects (green balls):
Li3BO3: Wyckoff sites 2b with coordinates (0.5, 0.5, 0.5); Ef = 1.25 eV
Li3BN2: Wyckoff sites 4e with coordinates (0.560, 0.279, 0.978); Ef = 1.23 eV
2x2x1 supercell of β-Li3BN2 (P21/c)

## Slide 7
Li ion vacancy migration analysis via Elastic Band Method1,2
Inequiv. Li
For I-vac and doped crystals:
For perfect crystals:
Recall Ef = 1.25 eV for Li3BO3 and 1.23 eV for Li3BN2.
F
C
Li3BO3
Li3BN2
1Jónsson et al., in Classical and Quantum Dynamics in Condensed Phase Simulations, edited by B. J. Berne, G. Ciccotti, and D. F. Coker (World Scientific, Singapore, 1998)
2Henkelman et al., J. Chem. Phys. 113, 9901-9904 (2000)

## Slide 8
Molecular dynamics simulations
NVE ensemble
968 K
996 K
998 K
1272 K
1259 K
1261 K
1254 K

## Slide 9
Ionic conductivities
Exp1: Ohta et al., J. of Power Sources 238, 53 (2013)
Exp2: Yamane et al., J. Solid State Chem. 71, 1 (1987)
Exp3: Shigeno et al., Solid State Ion. 339, 114985 (2019)
with
Materials | Analysis | Ea | σ (T = 300 K)
I-vac Li3BO3 | MD | 0.53 | 3.2 x 10-7
 | NEB | 0.38 | --
F-doped Li3BO3 | MD | 0.45 | 3.4 x 10-6
 | NEB | 0.72 | --
Polycrystalline Li3BO3 | Exp1 | 0.51 | 
Glassy Li3BO3 | Exp2 | 0.60 | 
Materials | Analysis | Ea | σ (T = 300 K)
I-vac Li3BO3 | MD | 0.53 | 3.2 x 10-7
 | NEB | 0.38 | --
F-doped Li3BO3 | MD | 0.45 | 3.4 x 10-6
 | NEB | 0.72 | --
Polycrystalline Li3BO3 | Exp1 | 0.51 | 
Glassy Li3BO3 | Exp2 | 0.60 | 
Materials | Analysis | Ea | σ (T = 300 K)
I-vac Li3BN2 | MD | 0.48 | 7.2 x 10-7
 | NEB | 0.30 (a)/0.81 (bc) | --
C-doped Li3BN2 | MD | 0.57 | 4.8 x 10-8
 | NEB | 0.40 (a)/1.02 (bc) | --
Polycrystalline Li3BN2 | Exp2 | 0.66 | 
Glassy-ceramic Li3BN2 | Exp3 | 0.56 | 
Materials | Analysis | Ea | σ (T = 300 K)
I-vac Li3BN2 | MD | 0.48 | 7.2 x 10-7
 | NEB | 0.30 (a)/0.81 (bc) | --
C-doped Li3BN2 | MD | 0.57 | 4.8 x 10-8
 | NEB | 0.40 (a)/1.02 (bc) | --
Polycrystalline Li3BN2 | Exp2 | 0.66 | 
Glassy-ceramic Li3BN2 | Exp3 | 0.56 | 
Li3BN2
Li3BO3

## Slide 10
Interfaces with Li metal anode
Li
B
N
O
2x1x1 supercell of Li3BN2 and 24 metallic Li ions in [001] direction.
σ(Li3BO3/Li) = 19 meV/Å2/Li
σ(Li3BN2/Li) = 0.11 meV/Å2/Li -- good compatibility
3x1x1 supercell of Li3BO3 and 24 metallic Li ions in [100] direction.
The interface energy:
Where σ denotes the strain factor.
a -- electrolytes; b -- Li
Reaction: R  P | ∆USL | ∆Fvib | ∆F
 | 0.19 | 0.07 | 0.26
 | 0.64 | 0.08 | 0.72
 | 1.91 | 0.06 | 1.97
 | 1.38 | 0.07 | 1.45
Predicted reactions:
Electrolyte
Interface
Electrolyte
Interface

## Slide 11
Summary
The imaginary phonon modes near the M point of the Brillouin zone suggested the structural instability of the reported tetragonal phase of α-Li3BN2.
The real α phase has an orthorhombic structure formed with twice as many formula units and very small adjustments of the fractional coordinates compared with the original analysis. Quasi-harmonic corrections further improve the comparisons with experiment.
Both NEB and MD simulations indicate that the Li ion migration in monoclinic crystals of Li3BO3 and β-Li3BN2 most likely proceeds via vacancy mechanisms.
To enhance the ionic conductivity, the practical methods include: 1) Varying the structural perfection to intentionally form poor-crystallinity material containing vacancy-interstitial defect pairs; 2) Substituting F for O in Li3BO3 and C for B in β-Li3BN2.
The plausible Li3BO3 /Li and β-Li3BN2/Li interfaces are found to be physically and chemically stable.

## Slide 12
Acknowledgements
Prof. Natalie A. W. Holzwarth
(Wake Forest University)
Dr. Zachary D. Hood
(Argonne National Laboratory)
DE-AC02-06CH11357
DMR-1940324
**Computations were performed on the Wake Forest University DEAC cluster, a centrally managed resource
with support provided in part by the University.