## Slide 1
Li14(PON3)2: Computational study of a possible
new electrolyte for Li ion batteries
Ahmad N.Al-Qawasmeh and N. A. W. Holzwarth*
Wake Forest University, Winston-Salem, NC, USA
*Research was supported by NSF DMR 1507942. Computations were performed on WFU’s DEAC cluster.

## Slide 2
• Density functional theory with LDA approximation
• PAW formalism using datasets generated with ATOMPAW code (Holzwarth et al. CPC 135, 329 (2001))http://pwpaw.wfu.edu
• Electronic structure calculations performed using QUANTUM ESPRESSO . (Giannozzi et al. JPCM 21, 394402 (2009);http://www.quantum-espresso.org
• Plane wave expansion for wave functions with |k+G|2 ≤ 64 Ry

## Slide 3
Solid Electrolyte materials

## Slide 4
(Du,PHYSICAL REVIEW B 81, 184106,2010)
LixPOyNz
(x=2y+3z-5)

## Slide 5
Li14 (PON3 )2O: Computational study of a possible new electrolyte for Li ion batteries
(Schnick,Eur. J. Inorg. Chem. 2015, 617-621 )
trigonal, P3 (no. 147)
PON3
Li2O
N
P
O
Li
The First LiPON material with PON3
Tetrahedra .

## Slide 6
(Schnick,Eur. J. Inorg. Chem. 2015, 617-621 )
trigonal, P3 (no. 147)
Li
O
P
N
Comparison of different LiPON materials
γ – Li3PO4 ,orthorhombic Pnma
(Du,Phys Rev B 76, 174302)
Li7PN4, cubic P43n (no. 218)
(Schnick ,J of solid state chemistry. 1990, 37,101 )

## Slide 7
Structure analysis

## Slide 8
Electronic structure calculation
The valence band states are characterized by the 2p states of O and
N together with bonding combination of P 3s and 3p states, while the
N 2p dominates the top of the valence bands of the Li14(PON3)2 .
The conduction band are characterized by the corresponding antibonding
states

## Slide 9
∆HD = - 2.88 eV
Li7PN4
LiPN2+2Li3N
∆HD = - 2.93eV
Li14P2O3N6
3Li2O + 2Li3N+2LiPN2
Energy
Compound
Products
Heat of decomposition calculation

## Slide 10
Li14(PON3)2 : Li ion migration analysis
I
2d
II
1a
Formation Energy of 0.32 eV which involves
the pair ( g’-I ) .

## Slide 11
Li14(PON3)2 : Li ion migration analysis
Vacancy mechanism

## Slide 12
Li14(PON3)2 : Li ion migration analysis
Interstitial mechanism

## Slide 13
Li7PN4 : Li ion migration analysis

## Slide 14
Li7PN4 : Li ion migration analysis

## Slide 15
Li ion migration summary
Material | Mechanism | Ef (eV) | Em (eV) | Em +1/2 Ef (ev) | EA (eV)
Li14(PON3)2 | Vacancy | 0.3 | 0.3 | 0.4 | 
Li14(PON3)2 | Kick-out | 0.3 | 0.6 | 0.7 | 
Li7PN4 | Vacancy | 1.9 | 0.3 | 1.3 | 0.48
Li7PN4 with O | Vacancy |  | 0.5 |  | 0.48
ϒ-Li3PO4 | Kick-out | 1.7 | 0.3 | 1.2 | 1.1 – 1.2
β-Li3PO4 | Kick-out | 2.1 | 0.4 | 1.5 | 
Simulation
Experimental

## Slide 16
Li14(PON3)2 : Interface with Vacuum
(001)N
(001)N
(001)O

## Slide 17
Li14(PON3)2 : Interface with Li

## Slide 18
Li14(PON3)2 : Interface with Li
(Lepley, PHYSICAL REVIEW B 92, 214201 (2015))

## Slide 19
Li14(PON3)2 : Interface with Li

## Slide 20
Li14(PON3)2 : Interface with Li

## Slide 21
Summary and Conclusions
This work report a computational study of the structural and electrolyte properties
of the Li14(PON3)2 and Li7PN4 solid electrolyte materials .
The conduction process for these LiPON materials was dominated by the vacancy
mechanism in comparison to the kick-out mechanism in the Li3PO4 .
The calculated range of the activation energies for the Li14(PON3)2 was found to be lower
than Li7PN4 and Li3PO4 indicating relatively good conduction properties .
Both Li14(PON3)2 and Li7PN4 have a stable interface with metallic Li .