## Slide 1
Structure and interface properties of the electrolyte material Li4P2S6*
Zachary D. Hood,a Cameron M. Kates,b,c and
N. A. W. Holzwarthb
aCenter for Nanophase Materials Sciences,
Oak Ridge National Laboratory, Oak Ridge, TN 37831,
bDepartment of Physics, Wake Forest University, Winston-Salem, NC, USA, 27109,
cCurrently attending the Pratt School of Engineering at Duke University
  *Supported by NSF Grant DMR-1105485. Computations were performed on WFU’s DEAC cluster. ZDH was supported by the HERE program at ORNL. Helpful discussion with Chengdu Liang, Gayatri Sahu, Hui Wang, Melanie Kirkham, Jong Keum, and E. Andrew Payzant at ORNL and William C. Kerr, Keerthi Senevirathne, Cynthia Day, and Abdessadek Lachgar at WFU are gratefully acknowledged.

## Slide 2
Li4P2S6
Why--
What--
Part of search for ideal solid electrolyte materials for all-solid state Li ion batteries
Reported in by Mercier et. al. , J. Solid State Chemistry 43, 151-164 (1982); hexagonal structure with disorder on the P sites
Frequently identified as unintended constituent of solid electrolyte preparations; relatively stability in air
Combined experimental and computation study including:
Structural analysis
Thermal stability
Transport properties

## Slide 3
Outline
  Motivation
  Structural analysis
  Thermal stability
  Ionic conductivity
  Summary and conclusions

## Slide 4
Motivation for studying Li4P2S6:
  Part of the search for the ideal solid electrolyte material for all-solid state Li ion batteries
  Li4P2S6 frequently identified as unintended stable component of solid electrolyte preparations
  Interesting structural properties, including disorder
  Transport and stability properties
Previous work:

## Slide 5
Synthesis:
Sulfur removed by treatment with solvent; sample prepared for electrochemical applications using ball milling.
Scanning Electron Micrograph of prepared sample:

## Slide 6
Computational methods
Density functional theory with LDA
PAW formalism using datasets generated with ATOMPAW code
Electronic structure calculations performed using QUANTUM ESPRESSO and ABINIT codes
Plane wave expansion for wave functions with
Brillouin zone integration mesh of 0.003 bohr-3
Visualization software: Xcrysden and VESTA; X-ray powder diffract simulated using Mercury

## Slide 7
Crystal structure: Space Group P63/mcm (#193)
Projection on to hexagonal plane:
a
a
S
P
Li

## Slide 8
Crystal structure: Space Group P63/mcm (#193)
Li4P2S6 units:
c
S
P
Li
2.3 Å
2.1 Å

## Slide 9
Crystal structure: Space Group P63/mcm (#193)
Disorder in P-P placements:
c
+z
-z
+(1/2-z)
-(1/2-z)
­
Site label z­
Site label z­ ­­­­­­
S
P
Li

## Slide 10
Structural variation can be mapped on to a two-dimensional hexagonal lattice with each P configuration taking z or z settings; Li and S configurations fixed
S
P
Li

## Slide 11
Examples:
Structure “b”
Structure “c”
Structure “d”
DE = 0
DE = 0
DE = 0.03 eV
100% z­ ­­­­­­
50% z
50% z­ ­­­­­­
50% z
50% z­ ­­­­­­
S
P
Li

## Slide 12
Temperature dependence of X-ray powder diffraction
in
^

## Slide 13
 | a (Å) | c (Å) | zP | zS
Exp. 298K (X-ray) | 6.0709 | 6.5903 | 0.1715 | 0.3237
Exp. 13K (X-ray) | 6.0747 | 6.5966 | 0.1715 | 0.3237
Exp. 13K (neutron) | 6.0761 | 6.5961 | 0.1698 | 0.3284
Diffraction analysis

## Slide 15
Comparison of 13 K
X-ray data with simulations
Note: simulations scaled by 102% to compensate for systematic LDA error.
Extra peaks
Simulations consistent with incoherent average over all P z and z
configurations

## Slide 16
Stability: Li4P2S6 is much less reactive than other lithium thio-phosphates, but it decomposes in air, especially at higher temperature
Decomposition products:
P2O5
Li4P2O7
Li2SO4

## Slide 17
Ionic conductivity and Activation Energy
2.38 x 10-7 S/cm at 25˚C and 2.33 x 10-6 S/cm at 100˚C
Li4P2S6 pressed pellets with blocking (Al/C) electrodes

## Slide 18
Simulations of ion mobility using Nudged Elastic Band Model
Vacancy mechanism:
DE>0.6 eV
Interstitial mechanism:
DE>0.1 eV
S
P
Li
Possible interstitial sites

## Slide 19
Models of Li4P2S6/Li interfaces -- Surface parallel to P-P bonds:
Surface with vacuum
Surface with lithium
S
P
Li

## Slide 20
Models of Li4P2S6/Li interfaces -- Surface perpendicular to P-P bonds:
Surface with vacuum
Surface with lithium
S
P
Li

## Slide 21
Conclusions:
  Diffraction results are consistent with Mercier’s 1982 analysis with disorder on P sites due to small energy differences of alignment of P2S6 fragments; remarkably temperature independent
  Small activation energy (Ea = 0.3 eV) for ion conductivity consistent with interstitial mechanism
  Thermal stability relative to other thio-phosphates
  Simulations of Li4P2S6/Li interfaces suggest that meta-stable buffer layers may be formed
  Further processing of materials needed to improve conductivity and stabilize Li/Li4P2S6/Li cells