## Slide 1
Computational Study of Ideal Electrolyte/Anode Interface for Na3SbS4/Na
Larry E. Rush Jr., N.A.W. Holzwarth
Department of Physics, Wake Forest University, Winston-Salem, NC 27109
*Thanks to Zach Hood from Georgia Tech and ORNL for introducing us to this system $$
NSF grant DMR-1507942

## Slide 2
Outline
Na-ion electrolytes for all-solid-state Na-ion batteries
Motivation behind studying Na3SbS4
Computational Methods
Results
Conclusions

## Slide 3
Na-ion Electrolytes
Abundant (geopolitically-neutral & cheap)
↑ size of Na ions = ↑ intercalation w.r.t. Li ions (higher reversibility)*
Cost-effective large-scale grid storage (option for Morocco’s energy initiative?)
High energy density
* https://ceder.berkeley.edu/research-areas/na-ion-battery-materials-design-and-discovery//

## Slide 4
                Why Na3SbS4?
Similar to Na3PSe41
Air-stable & high ionic conductivity2,3,4
at 25⁰C4
1. Ceder et al., Chem. Mater., 28, pp. 252-258 (2016)
2. Wang et al., Angew. Chem., 55, pp. 8551-8555 (2016)
3. Zhang et al., Adv. Sci., 3, pg. 1600089 (2016)$$$$$$
4. Banerjee et al., Angew. Chem., 55, pp. 9634-9638 (2016)

## Slide 5
Methodology
Density functional theory with local-density approximation (LDA)
Projector Augmented Wave (PAW) formalism
PAW basis and projector functions generated by ATOMPAW1
Quantum Espresso software package2
Density of States calculations
Nudged Elastic Band (NEB) calculations3
1. Holzwarth et al., Computer Physics Communications, 135, pg. 329 (2001)
2. Giannozzi et al., J. Phys.: Cond. Mat., 21, pg. 395592 (2009) $$$$$$$$$$
3. Henkleman et al., J. Chem. Phys., 113, pp. 9901-9904 (2001)$$$$$$$$$$$$

## Slide 6
                Results
Low temperature phase Na3SbS4 (space group P 21 c)
2b 8e 2a 4d
Sb S Na Na
Wyckoff labels
Atoms

## Slide 7
                Results
Ball-and-stick model for Na3SbS4
NEB calculations
Sb S Na Na
2b 8e 2a 4d
Wyckoff labels
Atoms
c-axis
a-axis
σ =
a-axis

## Slide 8
                Results
Initial Na3SbS4/Na interface
Interface Properties
Final Na3SbS4/Na interface
Na
(110) Na3SbS4
Na
(110) Na3SbS4
Na3SbS3?
Na2S?
Sb S Na

## Slide 9
Final Na3SbS4/Na interface
                Results
Initial Na3SbS4/Na interface
Na
(100) Na3SbS4
Na3SbS3?
(100) Na3SbS4
Na2S?
Na
Sb S Na

## Slide 10
                Results
Density of States (DOS)
Bulk materials DOS
(110) Na3SbS4/Na interface
(110) Na3SbS4/Na interface DOS
Sb S Na
Na3SbS4
Na3SbS3?
Na2S?
Na

## Slide 11
a
a
a
Bulk Na3SbS3 (space group P 21 3)
                Results
4a 12b 4a 4a 4a
Sb S Na Na Na
Wyckoff labels
Atoms

## Slide 12
                Results
4a 12b 4a 4a 4a
Sb S Na Na Na
Wyckoff labels
Atoms
Ball-and-stick model for Na3SbS3
NEB calculations
2
3
1
1
1
1
2
2

## Slide 13
                Conclusions
Na3SbS4 has Em ≈ 0.05 eV for a-axis migration
Na3SbS4 is reactive to Na
Na3SbS3 & Na2S form at the Na3SbS4/Na interface (based on DOS)
Pure Na3SbS3 has Em ≈ 0.4 eV

## Slide 14
Acknowledgements
This work was supported by NSF grant DMR-1507942. Computations were performed on the Wake Forest University HPC DEAC Cluster.
Special thanks to Prof. Natalie Holzwarth
Thank you for your attention!