## Slide 1
First principles simulations of electrolyte materials with a view toward all solid-state battery technology --
Li4P2S6, Na4P2S6, and possible alloys
Yan Li1, Zachary Hood2, and Natalie Holzwarth1
1Department of Physics, Wake Forest University
2Electrochemical Materials Laboratory, MIT; now at
Argonne National Labs
WFU effort supported by Deac Cluster and
NSF Grants DMR-1507942 and 1940324.
Zach, Natalie, and Yan posing at 256th Meeting of the Electrochemical Society in Atlanta, GA Oct. 12-17, 2019
Contributions from previous students including Larry Rush and Cameron Kates are also gratefully acknowledged.
Ref: PRM 4, 045406 (2020)

## Slide 2
Outline
Motivation
Experimental story
Computational story
Outlook

## Slide 3
Motivation
  Research on battery materials
  The case for all solid state batteries
  Challenges for realistic (idealistic??) computer modeling

## Slide 4
Motivation
  Research on battery materials
Materials components of a Li or Na ion battery
+
-
Li+ or
Na+
Illustrating discharge mode
Role of the electrolyte is to allow for the transport of Li+ or Na+ ions, excluding electrons from the battery and forcing them through the external circuit.

## Slide 5
Motivation
  The case for all solid state batteries
Development of LiPON electrolyte films at Oak Ridge National Laboratory

## Slide 6
Motivation -- The case for all solid state batteries
  Advantages
Compatible and stable with high voltage cathodes
Compatible and stable with Li metal anodes
Can be effective in thin formats
  Disadvantages
Relatively low ionic conductivity
Lower total capacity compared with liquid electrolytes
Possible physical and chemical interface issues
Demonstrated for LiNi0.5Mn1.5O4/LiPON/Li
  10-6 m LiPON electrolyte layer achieved adequate conductivity
  10,000 cycles* with 90% capacity retention
*1 cycle per day for 27 years
ORNL

## Slide 7
Motivation
  Challenges for realistic (idealistic??) computer modeling
    Technological challenges –
      Improving the ionic conductivity
      Stabilizing the electrolyte material in battery conditions
      Stabilizing the cathode/electrolyte and anode/electrolyte interfaces
    Checking accuracy of computational models in terms of physical and numerical approximations, comparing with real materials

## Slide 8
Experimental story – Li4P2S6 and Na4P2S6 as examples of interesting electrolyte systems
Li4P2S6 has been identified as a low conductivity decomposition product in the formation of lithium thiophosphate electrolytes.

## Slide 9
Minami et al. 2010, continued
Li7P3S11
Li4P2S6
Li7P3S11
Li4P2S6

## Slide 10
Experimental story – Li4P2S6 continued --
Structure analyzed as a disordered hexagonal structure with space group P63/mcm (#193)

## Slide 11
Experimental story – Li4P2S6 continued --
P2S64- building blocks:
S
P
Mercier’s disordered structure ascribed to placement of the building blocks and the corresponding arrangement of Li ions.
hexathiohypodiphosphate

## Slide 12
Experimental story – Li4P2S6 continued --
Prepared more highly crystalline samples; combined NMR and X-ray analysis to show that there are two inequivalent P sites

## Slide 13
Experimental story – Li4P2S6 continued --
Neuberger structure
ordered structure
reported as P321
Space group
P321  P3m1
_
S
P
Li
our simulations

## Slide 14
Experimental story – Na4P2S6 continued --
Na4P2S6 found to crystallize in a base centered monoclinic structure with space group C2/m (#12); result verified by Zachary Hood and colleagues who also found the material to have appreciable Na ion conductivity.

## Slide 15
Experimental story – Na4P2S6 continued --
Primitive cell of the Kuhn structure
Space group C2/m
S
P
Na

## Slide 16
Computational challenges –
  Can computer modeling explain the structural stability patterns found by experiment?
  What about possible new related materials?
  What does computer modeling say about the mechanisms of ionic conductivity?

## Slide 17
  Simulation of structural stability patterns
Computational details –
  Formalism: Born-Oppenheimer approximation + Density functional theory (Hohenberg and Kohn, Phys. Rev. 136 B864 (1964); Kohn and Sham, Phys. Rev. 140 A1133 (1965))
  Method: Projector Augmented Wave (P. Blöchl, Phys. Rev. B 50 17953 (1994))
  Exchange correlation function: PBEsol (Perdew et al., PRL 100 136406 (2008))
Codes used for calculations
Function | Code | Website
Generate atomic datasets | ATOMPAW | http://pwpaw.wfu.edu
DFT; optimize structure; vibrational analysis | PWscf abinit | http://www.quantum-espresso.org http://www.abinit.org
Structural visualization | XCrySDen VESTA | http://www.xcrysden.org http://jp-minerals.org/vesta/en/

## Slide 18
Simulation of structural stability patterns -- continued
Static lattice
approx
Harmonic phonon approx
Internal energy from DFT
phonon DOS

## Slide 19
Simulation of structural stability patterns -- continued
1Suggested path: Hinuma et al., Comp. Mat. Sci. 128, 140-184 (2017)
2Li et al., J. Phys. Condens. Matter, 32, 055402 (2020)
Na4P2S6 in the C2/m Structure (36 modes)
PJDOS:
Na+ 0~300 cm-1
(P2S6)4- 370~600 cm-1
Li4P2S6 in the Pm1 Structure (108 modes)
Li+ 0~370 cm-1
(P2S6)4- 300~600 cm-1
Discontinuous branches at Г: coupling between photon and photon2

## Slide 20
USL: Pm1 < P1m < C2/m
Fvib: C2/m < Pm1 = P1m
Fvib: C2/m < Pm1 = P1m
USL: Pm1 = C2/m < P1m
Flowest: Pm1 (expt.3)
Flowest: C2/m (expt.1,2)
1Kuhn et al., Z. Anorg. Allg. Chem. 640, 689-692 (2014)
2Hood et al., J. Solid State Ionics 284, 61 (2016)
3Neuberger et al., Dalton Trans. 47, 11691-11695 (2018)
Helmholtz free energy:
F = USL + Fvib
Simulation of structural stability patterns -- continued

## Slide 21
Simulation of structural stability patterns -- continued
Summary of simulation energies
Na4P2S6 | DUSL(eV) | Fvib(300K)(eV) | F(300K)(eV)
Neuberger structure (P3m1) | 0.00 | -0.04 | -0.04
Kuhn structure (C2/m) | 0.00 | -0.08 | -0.08
Simple hex structure (P31m) | 0.09 | -0.04 | 0.05
Li4P2S6 | DUSL(eV) | Fvib(300K)(eV) | F(300K)(eV)
Neuberger structure (P3m1) | 0.00 | 0.19 | 0.19
Kuhn structure (C2/m) | 0.31 | 0.12 | 0.43
Simple hex structure (P31m) | 0.04 | 0.20 | 0.24
_
_
_
_
Energies given in units of eV/formula unit with zero set at the static lattice energy for the Neuberger structure.

## Slide 22
Some details of the vibrational stabilization

## Slide 23
Some details of the vibrational stabilization

## Slide 24
Some details of the vibrational stabilization

## Slide 25
Some details of the vibrational stabilization

## Slide 26
Some details of the vibrational stabilization at T=300K for Li4P2S6 and Na4P2S6 in C2/m structure
~
~
Fvib(300K)=-0.08 eV
Fvib(300K)=0.12 eV

## Slide 27
Na ion conductivity of Na4P2S6 and Li2Na2P2S6 in the C2/m structure
Conducting plane for Na ions
Predicted Li2Na2P2S6 has Li ions at these g sites.

## Slide 28
Na ion conductivity of Na4P2S6 and Li2Na2P2S6 in the C2/m structure
View of mobile Na ion plane (h plane)
host Na site
interstitial Na site

## Slide 29
Computer modeling of mechanisms of ionic conductivity; comparing Na4P2S6 and Li2Na2P2S6 --
Li2Na2P2S6
Na4P2S6
MD simulations at <T>=1000K; Na ion motion in h planes --

## Slide 30
  Ionic conductivity

## Slide 31
  Ionic conductivity

## Slide 32
  Summary
Na4P2S6
Li4P2S6
Poor ionic conductor
Structure stabilized by static lattice energy
Good ionic conductor within plane
Structure stabilized by vibrational energy

## Slide 33
  More thoughts
DFT with PBEsol+harmonic phonon simulations agree with the experimental structures of Na4P2S6 (space group C2/m found by Kuhn and Hood) and Li4P2S6 (space group Pm1, close to that found by Neuberger).
For Na4P2S6 find Na+ migration to take place in planes with the h-sites via a vacancy mechanism, involving interstitial d-sites. Both simulations and experiment suggest that Na4P2S6 may be a viable solid electrolyte.
Simulations predict Li2Na2P2S6 to crystallize with the C2/m structure and to be stable relative to Na4P2S6+2Li-2Na. The mixed alkali electrolyte is predicted to substantially enhance Na ion conductivity.
In addition to experimental verification (or otherwise) of the predictions for Li2Na2P2S6, further MD simulations for both Na4P2S6 and Li2Na2P2S6 will help us better understand Na ion conductivity mechanisms.