## Slide 1
Prediction and analysis of a sodium ion electrolyte: Li2Na2P2S6
Yan Li1, Zachary D. Hood2 and Natalie A. W. Holzwarth1
1Department of Physics, Wake Forest University, Winston-Salem, NC 27109, USA
2Electrochemical Materials Laboratory, MIT, Cambridge, MA 02139, USA
Acknowledgements: This work is supported by NSF grant DMR-1507942. Computations were performed on the Wake Forest University DEAC cluster, a centrally managed resource with support provided in part by the University.

## Slide 2
Three focuses of submitted work “Computational and experimental (re)investigation of the structural and electrolyte properties of Li4P2S6, Na4P2S6, and Li2Na2P2S6” by Yan Li, Zachary D. Hood, and N. A. W. Holzwarth,
Crystal structure stabilities of Li4P2S6 and Na4P2S6
This talk:
Structure and stability of predicted mixed ion electrolyte Li2Na2P2S6
Performance of Li2Na2P2S6 in comparison with Na4P2S6 as solid electrolytes
The Helmholtz free energy:
Ground state structure:
Na4P2S6 : Monoclinic C2/m (#12)
Li4P2S6: Hexagonal Pm1 (#164)
Outline
1Neuberger et al., Dalton Trans. 47, 11691-11695 (2018)
2Kuhn et al., Z. Anorg. Allg. Chem. 640, 689-692 (2014)
3Hood et al., Manuscript in preparation.
consistent with those experiment results1-3
See more at http://users.wfu.edu/natalie/presentations/
Notes: My talk is based on our recently submitted work “Computational and experimental (re)investigation of the structural and electrolyte properties of Li4P2S6, Na4P2S6, and Li2Na2P2S6” which has three main focuses. In the first part of the work, we showed that the enhanced computational methods with consideration of phonon contributions can explain the experimentally observed structures of Na4P2S6 and its Li4P2S6 analog.
Studies on these two materials also prompt an investigation of their alloys, one of them has composition Li2Na2P2S6. The following slides will show the predicted structures of this mixed ion material and the stability analysis in terms of reaction energies of proposed reaction pathways. Also the electrolyte properties of Li2Na2P2S6 will be discussed in comparison with those of Na4P2S6.

## Slide 3
Density Functional Theory (DFT) and Density Functional Perturbation Theory (DFPT) with the modified Perdew-Burke-Ernzerhof generalized gradient approximation1 (PBEsol GGA)
The projector augmented wave (PAW) formalism using ABINIT (https://www.abinit.org) & QUANTUM ESPRESSO (http://www.quantum-espresso.org)
Datasets generated by ATOMPAW code available at http://pwpaw.wfu.edu
Visualization software: XCrySDen, VESTA
Space-group analysis: FINDSYM
X-ray powder diffraction: Mercury
1Perdew et al., Phys. Rev. L. 100, 136406 (2008)
Summary of computational methods
Notes: The computational methods are based on Density Functional Theory (DFT) and Density Functional Perturbation Theory (DFPT) using the Projector Augmented Wave (PAW) formalism. The PAW basis and projector functions were generated by the ATOMPAW code and used in both the ABINIT and QUANTUM ESPRESSO packages. In the present work, the PBEsol GGA was used to treat the exchange and correlation effects.

## Slide 4
The prototypic structure
1Kuhn et al., Z. Anorg. Allg. Chem. 640, 689-692 (2014)
2Hood et al., Manuscript in preparation.
Na4P2S6 crystallizes in a base-centered monoclinic structure with space group C2/m (#12)1,2 and this material was also found to have appreciable Na ion conductivity (3x10-6 S/cm) at room temperature2.
Primitive cell with 12 atoms/formula unit
interlayer plane
intralayer plane
h-type Na
(P2S6)4- units
with D3d symmetry
g-type Na
Notes: This diagram shows the ball and stick model of the C2/m structure in primitive cell setting, in which the P2S6 building blocks aligned orderly and uniformly throughout the space. Such structural framework may benefit the diffusions of Na ions in the material.
As what we see this structure has two crystallographically distinct Na sites with Wyckoff labels g and h, respectively. Each g-type Na ion is located in an intralayer plane which contains the P2S6 units, while each h site Na ion is located in an interlayer plane between the P2S6 units. Staring with the monoclinic structure of the pure Na material, we predicted the possible structures of the mixed ion material Li2Na2P2S6 based on the idea of ionic substitution.

## Slide 5
Structures of the predicted material: Li2Na2P2S6
Replace the (a) g-type or (b) h-type Na ions in the monoclinic Na4P2S6 with Li ions
Na
Li
g sites
h sites
TABLE: Comparison of the optimized lattice parameters for Li2Na2P2S6 in the and structures. Also listed is the static lattice energy differences USL referenced to the energy of the structure in units of eV/formula unit.
Primitive cell: | a = b (Å) | 6.18 | 6.46
 | c (Å) | 7.50 | 7.01
 | α = β (deg) | 97.77 | 97.88
 | γ (deg) | 119.21 | 118.43
Conventional | ac (Å) | 6.26 | 6.61
cell: | bc (Å) | 10.67 | 11.10
 | cc (Å) | 7.50 | 7.01
 | βc (deg) | 105.50 | 105.54
 | ∆USL (eV/FU) | -0.16 | 0.00
Primitive cell: | a = b (Å) | 6.18 | 6.46
 | c (Å) | 7.50 | 7.01
 | α = β (deg) | 97.77 | 97.88
 | γ (deg) | 119.21 | 118.43
Conventional | ac (Å) | 6.26 | 6.61
cell: | bc (Å) | 10.67 | 11.10
 | cc (Å) | 7.50 | 7.01
 | βc (deg) | 105.50 | 105.54
 | ∆USL (eV/FU) | -0.16 | 0.00
in interlayer
in intralayer
Notes: The left diagram illustrates one likely geometry of atomic arrangements, generated by replacing all equivalent Na ions at g sites with Li ions. And by substituting the Li ions for all h-type Na ions in interlayer planes, we obtain another possible atomic configuration .
After optimization, we found both proposed structures retain their space group symmetry C2/m. For the reason that results in a lower static energy structure relative to , the configuration is determined to be the ground state structure of Li2Na2P2S6 and will be used in subsequent analysis and simulations.
The left diagram illustrates one likely geometry 𝑅_𝑔^𝐿𝑖 of atomic arrangements, generated by replacing all equivalent Na ions at g sites with Li ions. And by substituting the Li ions for all h-type Na ions in interlayer planes, we obtain another possible atomic configuration 𝑅_ℎ^𝐿𝑖.
After optimization, we found both proposed structures retain their space group symmetry C2/m. For the reason that 𝑅_𝑔^𝐿𝑖 results in a lower static energy structure relative to 𝑅_ℎ^𝐿𝑖, the configuration 𝑅_𝑔^𝐿𝑖 is determined to be the ground state structure of Li2Na2P2S6 and will be used in subsequent analysis and simulations.

## Slide 6
Comparison of phonon spectra
Na4P2S6 in the C2/m Structure (36 modes)
Li2Na2P2S6 in the C2/m Structure (36 modes)
1Suggested path: Hinuma et al., Comp. Mat. Sci. 128, 140-184 (2017)
2Li et al., J. Phys. Condens. Matter, 32, 055402 (2019)
PJDOS:
Discontinuous branches at Г: coupling between photon and photon2
(P2S6)4- 300~600 cm-1
Na+ 0~300 cm-1
Li+ 0~320 cm-1
evidence of dynamical stability
Notes: Here we see that phonon dispersion curves of the two materials are very similar with the same number of modes covering an almost identical range of frequencies. For the case of Li2Na2P2S6 , the fact of having all real phonon frequencies implies that its possible ground state structure is dynamically stable.
As highlighted by short red arrows, there are several branches that are not continuous functions of q near gamma point. The physical reason for this kind of discontinuity is explained in terms of the coupling between the optical phonon modes and the electromagnetic field. For some of you who interest in such coupling effects, detailed discussions can be found in our published paper “Li et al., J. Phys. Condens. Matter, 32, 055402 (2019)”.

## Slide 7
Stability of the predicted material: Li2Na2P2S6
The possible reaction pathway:
Energy changes at T = 300 K in eV:
trivial contribution
(10-3 eV)
Negative energies (net released energies) implies that the products Li2Na2P2S6 + 2 Na is stable with respect to the reactants Na4P2S6 + 2 Li.
Notes: To further evaluate the stability of this predicted alloyed material Li2Na2P2S6, we proposed this possible reaction pathway and calculated the reaction energy which is determined from the energy difference between the right side products and the left-side reactants. For each component, the energy of it is obtained from the sum of static and vibrational contributions. In particular for Li and Na in their metallic form, we also considered the energy due to the temperature-dependent excitations, but it turns out this contribution is very small compared to others and can be neglected.
It shows that at room temperature, the reaction energy is -0.35 eV. The figure on the right demonstrates that the reaction energy is gradually decreasing along with the increasing temperature, suggesting that it is energetically favorable for Li to replace Na according to this reaction over a significant temperature range.

## Slide 8
More possible reaction pathways
a Black phosphorous with Space Group Cmce (#64); from Brown et al. Acta Cryst. 19, 684 (1965).
b Orthorhombic (α-S8) with Space Group Fddd (#70); from S. J. Rettig and J. Trotter, Acta Cryst. C 43, 2260 (1987).
c γ-Li3PS4 with Space Group Pmn21 (#31); from Homma et al., Solid State Ionics 182, 53 (2011).
d α-P4S4 with Space Group C2/c (#15); from Minshall et al., Acta Cryst. B 34, 1326 (1978)..
e α-Na3PS4 with Space Group P421c (#114); from Jansen et al., J. Solid State Chem. 99, 110 (1992).
f P4S10 with Space Group P (#2); from Vos et al., Acta Cryst. 19, 864 (1965).
TABLE: Computed energy differences for indicated reactions in eV units, evaluated
at T = 300 K and neglecting electronic excitation contributions.
Notes: Besides the possible synthesis route given in the previous slide, there are a number of other possible reactions we can imagine to produce the mixed ion electrolyte Li2Na2P2S6. In this table, we summarized the room-temperature reaction energies for some of those pathways. Here we see that the only reaction that has a positive reaction energy ∆F is reaction No. 3, which means the mixed material is unstable relative to these two left-side reactants. But we also learn from the experiment that the pure Li material Li4P2S6 forms at very high temperatures, which implies that it is still possible to produce Li2Na2P2S6 via a low-temperature synthesis process with the metal-stable phase of Li4P2S6 as one of the reactants.

## Slide 9
Ion migration of vacancy mechanisms
Activation energy:
Na (h)
P
S
Na/Li (g)
Configuration energy diagram results of NEB calculation of Na ion vacancy migration along one step of the indicated pathway.
interlayer plane
Interstitial d site
Nudged Elastic Band1 algorithm
1Henkelman et al., J. Chem. Phys. 113, 9901-9904 (2000)
Notes: To understand the conductivity properties of the mixed ion material Li2Na2P2S6 in comparison with the pure Na material Na4P2S6, we investigated the diffusion mechanisms and estimated the related activation energy Ea for Na ions hopping for both materials. And among many possible migrating paths, we identified that the most favorable path for Na ion vacancy migration appears to be between h sites. When viewing down the c axis, we would see the hops from one host h site to the adjacent vacancy construct a continuous zig-zag path from one side of the crystal structure to another. The resulted NEB diagram between such two local minimum energy configurations shows that the energy barrier of the mixed material is lower by about 0.1 eV than of the pure Na material.
Within this methodology, the activation energy Ea of the perfect crystal includes both migration energy Em and also the formation energy Ef which is associated with the creation of a vacancy-interstitial pair (defect). In this diagram, the extra gray balls represent the interstitial d sites from which the defect formation energy Ef is determined.

## Slide 10
Migration study using molecular dynamics simulations
No and hopping
All migrations occur within interlayer plane containing h-type Na ions
Direct vacancy migration is consistent with NEB analysis
Indirect vacancy migration is prevalent
No interstitial migration
*AIMD simulations were carried out using supercells composed of 2x1x2 conventional units (96 atoms)
Na4P2S6
Li2Na2P2S6
Extra interstitial d site
Host h site
interlayer plane
at T = 1000 K
Both Na ion vacancy sites and indirect participation of interstitial sites contribute to the conductivity throughout the interlayer plane
Notes: By directly observing the trajectories of atoms produced by molecular dynamics simulations, we found that for both materials all migration events only occur within the interlayer plane containing all h sites. Here we have movies for visualizing the trajectories of h-type Na ions at T = 1000K. At the beginning of the calculation, there are 8 Na ions resided at each interlayer plane in the simulation cell. More balls were placed to display that the Na ion may migrate to the neighboring cells.
Note in this document, the animations were represented by the superposed snapshots of the ion positions at t =~10 ps, ~15 ps and ~30 ps as presented in the next 3 slides.

## Slide 11
Migration study using molecular dynamics simulations
No and hopping
All migrations occur within interlayer plane containing h-type Na ions
Direct vacancy migration is consistent with NEB analysis
Indirect vacancy migration is prevalent
No interstitial migration
*AIMD simulations were carried out using supercells composed of 2x1x2 conventional units (96 atoms)
Na4P2S6
Li2Na2P2S6
Extra interstitial d site
Host h site
interlayer plane
at T = 1000 K
Both Na ion vacancy sites and indirect participation of interstitial sites contribute to the conductivity throughout the interlayer plane
Notes: Qualitatively speaking, compared to the case for Na4P2S6 the Na ions migrate more frequently in the mixed material Li2Na2P2S6, presenting a more extensive network of diffusional channels. To quantify these effects, we analyzed the nearest-neighbor hopping events, that is, the average number of hops between nearest neighboring sites, as a function of time. The story we can tell from the plots of H vs t is that for each material, the Na ion diffusion is either via direct vacancy mechanism between h to h, or via indirect vacancy mechanism between h to d or d to h. The h to d hops are more prevalent than the h to h hops, suggesting the interstitial d sites play an important role as intermediates in the Na ion migration processes throughout the interlayer plane.

## Slide 12
Migration study using molecular dynamics simulations
No and hopping
All migrations occur within interlayer plane containing h-type Na ions
Direct vacancy migration is consistent with NEB analysis
Indirect vacancy migration is prevalent
No interstitial migration
*AIMD simulations were carried out using supercells composed of 2x1x2 conventional units (96 atoms)
Na4P2S6
Li2Na2P2S6
Extra interstitial d site
Host h site
interlayer plane
at T = 1000 K
Both Na ion vacancy sites and indirect participation of interstitial sites contribute to the conductivity throughout the interlayer plane

## Slide 13
Migration study using molecular dynamics simulations
No and hopping
All migrations occur within interlayer plane containing h-type Na ions
Direct vacancy migration is consistent with NEB analysis
Indirect vacancy migration is prevalent
No interstitial migration
*AIMD simulations were carried out using supercells composed of 2x1x2 conventional units (96 atoms)
Na4P2S6
Li2Na2P2S6
Extra interstitial d site
Host h site
interlayer plane
at T = 1000 K
Both Na ion vacancy sites and indirect participation of interstitial sites contribute to the conductivity throughout the interlayer plane

## Slide 14
Ionic conductivity (continued)
TABLE: NEB and MD results calculated with the PBEsol exchange-correlation functional, in comparison to those of previous work obtained using the LDA exchange-correlation functional and available experimental data. All energies are given in eV units.
Molecular dynamics analysis of the ionic conductivity. The activation energy is obtained from the slope of the corresponding fit line.
Materials | Analysis | Em | Ef | Ea
Na4P2S6 | LDA + NEB1 | 0.30 | 0.24 | 0.42
 | PBEsol + NEB | 0.25 | 0.18 | 0.34
 | PBEsol + MD | -- | -- | 0.41
 | Experiment2 | -- | -- | 0.39
Li2Na2P2S6 | PBEsol + NEB | 0.16 | 0.13 | 0.23
 | PBEsol + MD | -- | -- | 0.30
Li2Na2P2S6 presents better Na ion conductivity than Na4P2S6
1Rush et al., Solid State Phys. 286, 45-50 (2016)
2Hood et al., Manuscript in preparation.
Notes: Both NEB and molecular dynamics analyses suggest that the mixed ion material Li2Na2P2S6 has lower activation barriers and larger conductivity compared with Na4P2S6. The present computational results on Na4P2S6 are in reasonable agreement with the available calculated results using LDA in Ref. 1 and the experimental measurement in Ref. 2.
We also noticed that for these systems, ≠ because of their different treatments of the effects of interstitial d sites. The NEB analysis presented here only considered direct hops between nearest neighbor vacancy sites, including the interstitial sites only in the estimation of the population of vacancies via the Boltzmann factor due to the formation energy Ef of the interstitial-vacancy pair. The molecular dynamics results indicate significant contributions of hops between vacancy and interstitial sites, presenting a plausibly more physical picture of the Na ion migration processes.
Both NEB and molecular dynamics analyses suggest that the mixed ion material Li2Na2P2S6 has lower activation barriers and larger conductivity compared with Na4P2S6. The present computational results on Na4P2S6 are in reasonable agreement with the available calculated results using LDA in Ref. 1 and the experimental measurement in Ref. 2.
We also noticed that for these systems, 𝐸_𝑎^𝑁𝐸𝐵≠ 𝐸_𝑎^𝑀𝐷 because of their different treatments of the effects of interstitial d sites. The NEB analysis presented here only considered direct hops between nearest neighbor vacancy sites, including the interstitial sites only in the estimation of the population of vacancies via the Boltzmann factor due to the formation energy Ef of the interstitial-vacancy pair. The molecular dynamics results indicate significant contributions of hops between vacancy and interstitial sites, presenting a plausibly more physical picture of the Na ion migration processes.

## Slide 15
Summary
Using first-principle computational tools, we predicted the structure of a possible mixed ion material Li2Na2P2S6 and analyzed its stability in terms of Helmholtz free energies of proposed reaction pathways.
Conductivity studies on both Na4P2S6 and Li2Na2P2S6 indicates that Na ions move primarily within the interlayer region between the (P2S6)4- layers, efficiently proceeding via direct or indirect hops between vacancy sites, with indirect processes involving intermediate interstitial sites.
Li2Na2P2S6 has larger conductivity and lower activation barriers compared with Na4P2S6, suggesting that the predicted material to be more promising Na ion electrolytes.