## Slide 1
PHY 752 Solid State Physics
11-11:50 AM MWF Olin 107
Plan for Lecture 31:
      X-ray and neutron diffraction in solids (some material contained in Chap. 3 of Marder’s text)
        Bragg law
        Intensity relationships
        Sensitivity to atomic parameters

## Slide 3
Comment on topics
  X-ray and neutron diffraction in solids
  Low energy electron diffraction in solids
  Beyond independent electron picture -- Electron-electron interactions in the Hubbard model (Chapter 26 of your text)

## Slide 4
Bragg diffraction
incident beam
defracted beam
In terms of wave vectors
kinc
kscat
Dk
2q

## Slide 5
Relationship of normal distance between diffracting planes to Bravais lattice
a1
a2
a3

## Slide 6
Intensity profile
Comes from Born approximation describing the interaction between scattering particle and material.

## Slide 7
Atomic structure factors
For X-ray scattering; Fourier transform of electronic density
(these are from
crystaldiffract)

## Slide 8
Atomic structure factors
http://www.ncnr.nist.gov/resources/n-lengths/

## Slide 9
scattering length in 10-15 m

## Slide 10
Cu (fcc)

## Slide 11
X-ray powder diffraction pattern for Cu (fcc)
what is lattice constant a?
3.615 Angstroms

## Slide 12
Fe (bcc)

## Slide 13
Fe (bcc)
What is a ?
2.8665 Angstroms

## Slide 14
NaCl

## Slide 15
NaCl
a=5.6573 Angstroms

## Slide 16
Comparison of X-ray and Neutron diffraction
time of flight
path length

## Slide 17
X-ray
Neutron

## Slide 19
X-ray

## Slide 20
Properties of scattering particles
from pg. 61 of Marder’s text