## Slide 1
PHY 712 Electrodynamics
9-9:50 AM MWF Olin 103
Plan for Lecture 34:
    Special Topics in Electrodynamics:
    Electromagnetic aspects of superconductivity

## Slide 4
Special topic: Electromagnetic properties of superconductors
Ref:D. Teplitz, editor, Electromagnetism – paths to research,
Plenum Press (1982); Chapter 1 written by Brian Schwartz and Sonia Frota-Pessoa
History:
  1908 H. Kamerlingh Onnes successfully liquified He
  1911 H. Kamerlingh Onnes discovered that Hg at 4.2 K has vanishing resistance
  1957 Theory of superconductivity by Bardeen, Cooper, and Schrieffer

## Slide 5
Some phenomenological theories < 1957

## Slide 7
Some phenomenological theories < 1957

## Slide 8
London model – continued

## Slide 9
London model – continued
x
lL

## Slide 10
Magnetization field
At T=0K

## Slide 11
Magnetization field (for “type I” superconductor)
H
B
HC
-4pM
HC
GS-GN
HC
H
H

## Slide 12
characteristic phonon energy
density of electron states at EF
attraction potential between electron pairs

## Slide 13
Temperature dependence of critical field
From PR 108, 1175 (1957)
  Bardeen, Cooper, and Schrieffer, “Theory of Superconductivity”
characteristic phonon energy
density of electron states at EF
attraction potential between electron pairs

## Slide 14
Type I elemental superconductors
http://wuphys.wustl.edu/~jss/NewPeriodicTable.pdf

## Slide 15
Behavior of superconducting material – exclusion of magnetic field according to the London model
x
lL

## Slide 16
Behavior of magnetic field lines near superconductor
normal
state:
superconducting state:

## Slide 18
Type I superconductors:

## Slide 19
Type II superconductors

## Slide 20
Quantization of current flux associated with the superconducting state (Ref: Ashcroft and Mermin, Solid State Physics)

## Slide 21
Quantization of current flux associated with the superconducting state -- continued
dl
Suppose a superconducting material has a cylindrical void. Evaluate the integral of the current in a closed path within the superconductor containing the void.
Such “vortex” fields can exist within type II superconductors.

## Slide 23
Crystal structure of one of the high temperature superconductors

## Slide 24
Some details of single vortex in type II superconductor

## Slide 25
Scanning probe images of vortices in YBCO at 22 K